## Slide 1
EPI-Hi Technology Development

## Slide 2
Outline
objective
approach
development strategy and status
fidelity of test article
test performed
transition to flight

## Slide 3
Objective
Develop new approach to fabricating multi-element ion-implanted silicon solid-state detectors thinner than ~30μm with the following features:
thicknesses in the range ~10 to 30 μm
good control of absolute thickness and detector-to-detector variation (±1 μm)
good thickness uniformity (~0.2% or better rms variation) to allow good species resolution (e.g., He isotope separation)
mechanical robustness to provide good manufacturing yield and to survive launch environment without breaking

## Slide 4
Approach
fabrication based on commercial silicon-on-insulator wafers (SOI)
detector pn junctions produced on device layer of SOI using conventional ion-implantation technology
supporting handle layer etched away under portion of the wafer containing detector active area
thin SiO2 interface between the two wafers acts as etch stop that makes thickness control and uniformity independent of etch rate variations
remaining thick “picture frame” immediately outside the thinned region provides robust mechanical support and avoids the need to wirebond to the fragile thin membrane
production of ohmic contact and dicing into individual detectors done after thinning

## Slide 5
silicon-on-insulator (SOI) wafer, commercial product
ion implant to produce diode pn junctions on device layer
wet etch to remove handle layer under active area—oxide acts as etch stop
etch away oxide from underneath active area
ion implant from back to produce detector’s ohmic contact
dice wafer into individual thin detectors with thick supporting frames
thin device wafer
buried oxide
thick handle wafer
photoresist mask
nitride mask
Thin Silicon Detector Fabrication Process Summary

## Slide 6
PLACE-HOLDER SLIDE
SOI THICKNESS CHARACTERISTICS:
THICKNESS COMPARISON BETWEEN THINNED TEST SAMPLES OF SOI AND CONVENTIONAL (STEREO/LET) DETECTORS
MANUFACTURER DATA ON THICKNESS UNIFORMITY OF SOI PURCHASED FOR EPI-Hi THIN DETECTOR DEVELOPMENT

## Slide 7
Development Strategy and Status
Background
prototyping studies carried out by a collaboration between LBNL (diode fabrication) and Caltech/JPL since 2003
prior Caltech/JPL collaboration with Micron Semiconductor (Lancing, Sussex, England) allowed them to develop the capability for making thin, supported detectors from conventional silicon wafers; thickness control and uniformity were did not meet specifications
Phase B Activity
efforts to prototype EPI-Hi thin detectors from SOI wafers has been funded during phase B both at Micron and LBNL
testing and evaluation being carried out by the manufacturers and by Caltech/JPL and GSFC
Flight Detectors
plan to down-select to a single source for flight detectors based on test results

## Slide 8
PLACE-HOLDER SLIDE
Photograph of Thin Detectors
Labeling needed:
dimension
location of active area
comment about waviness
L0 Detector from
MIcron Semiconductor
L1 Detector from LBNL

## Slide 9
PLACE-HOLDER SLIDE
Photograph of SOI wafer after thinning

## Slide 10
Fidelity of the Test Article
flight detectors are expected to be identical to the prototypes
the same photolithography masks will be used
no changes are anticipated in process parameters (ion implantation energy, annealing temperature and time, etc.)
it presently appears that a sufficient supply of SOI wafers may be left over from the phase B work to allow fabrication of all of the flight detectors and spares
no changes are anticipated in the detector mounts (provided by GSFC to both LBNL and Micron)
possible exceptions
if expected risk from dust impacts is judged to be excessive, a modest increase in detector thickness (e.g., 12μm —> 15μm) could be considered
if LBNL is selected to make flight detectors, adhesive used for gluing detectors into mounts may be changed to that conventionally used by Micron

## Slide 11
Tests Performed
electrical characteristics
  leakage current versus bias (IV) —> maximum operating voltage
  capacitance versus bias (CV) —> bias required for full depletion
particle response
  alpha particles from 244Cm source (5.8 MeV —> 1.45 MeV/nuc)
  accelerator beams of heavy ions
thickness characteristics
  thickness and thickness uniformity inferred from particle response tests checked against expectations from SOI characteristics
stability in expected environment
  thermal-vacuum life test at GSFC—our standard test for flight qualification of all silicon detectors
  total dose testing using 60Co gamma-ray source at JPL
mechanical robustness
  acoustic test of mechanical model made from thinned SOI

## Slide 12
PLACE-HOLDER SLIDE
Plots of electrical characteristics
IV curve(s)
CV curve(s)
full-depletion voltage ~2V
breakdown voltage > 25V

## Slide 13
PLACE-HOLDER SLIDE
Acoustic Test of Mechanical Sample L0
silicon membrane
10 μm thick
~3.4 cm diameter
highest test level: 145 dB = SPP spec + 8 dB

## Slide 14
POSSIBLE PLACE-HOLDER SLIDE
PLOTS OF PARTICLE TEST RESULTS—ALPHAS
He mass histogram made using alpha particles—comparison with expected resolution
Possibly easier alternative to consider:
mono-energetic alpha particle ΔE and E’ distributions compared with expectations
NOTE: these data are not from EPI-Hi detectors; they are from a LBNL pre-prototype detector (15μm thick, 1cm2 active area, 4 pixels)
calibration pulser
241Am alpha ΔE

## Slide 15
PLACE-HOLDER SLIDE
PLOTS OF PARTICLE TEST RESULTS—HEAVY IONS
ΔE vs. E’ cross plot showing element tracks
NOTE: these data are not from EPI-Hi detectors; they are from 2007 test of Ortec thin surface barrier detectors at the LBNL 88-inch cyclotron

## Slide 16
Transition to Flight
extend selected prototype tests to cover additional detectors that have been fabricated in phase B—determine whether there are any detector-to-detector differences that might affect
  yield
  selection of manufacturer for flight detectors
  test program needed for flight devices
select manufacturer for flight detectors